NOTE TO USERS:  This document has been prepared for the LOGIX ICF one-sided insulated concrete form product, Logix ICF XP-1, and has been prepared in accordance with the Construction Specifications Institute (CSI) Section Format 2004.  The main intention of this document is to aid the Contractor/Installing Contractor in developing CSI specifications (of LOGIX ICF XP-1) for use in combination with specific project specification manuals, which follow CSI formatting, as part of the overall project scope of work.

This document is a template and where appropriate, may require modifications to suit specific projects.

Italicized text enclosed in parenthesis, { }, are intended for the user of this document to aid in determining where modifications may be required.}

##### PART 1 GENERAL

##### SUMMARY

- This section outlines the specifications for the implementation of LOGIX ICF XP-1, herein referred to as XP-1.

    - Section Includes

- XP-1 – one-sided permanent insulating concrete forming systems.

    - Products Supplied But Not Installed Under This Section

- Cast-in-place concrete

- EPS compatible waterproofing system

- EPS compatible parge coat

- Wall alignment system (wall bracing system)

    - Products Installed But Not Supplied Under This Section

- Service Penetration Sleeves

- Inserts

- Hold-Downs & Anchors

- Bolts

- Reinforcing Steel

- Window & Door Bucks (Openings)

- Concrete

- XP-1 products or components that are installed by owner or by others shall comply with Division 1 as required.

- The Installing Contractor shall furnish all labor, materials, tools and equipment to perform the installation of LOGIX ICF, including placement of reinforcing steel, placement of concrete and final cleanup.

    - Related Sections

{NOTE: This section may be modified to suit specific project details.}

- Section 03 20 00: Concrete Reinforcement

- Section 03 11 13: Structural Cast-In-Place Concrete Forming

- Section 03 30 00: Cast-in-place Concrete

- Division 04 00 00: Masonry

- Division 05 00 00: Metals

- Division 06 00 00: Woods, Plastics, and Composites

- Section 07 13 00: Sheet Waterproofing

- Section 07 24 00: Exterior Insulation Finishing Systems

- Section 07 46 00: Siding

- Division 08 00 00: Doors & Windows

- Division 09 22 00 – 09 25 00: Supports for Plaster and Gypsum Board – Other Plastering

- Section 09 70 00 – 09800: Wall Finishes - Acoustical Treatments

    - Alternates

- Unless otherwise approved by owner or owner’s Engineer or Architect, alternate materials or similar products shall not be accepted.  Alternates or similar products are materials or products that are not specified within this document and/or do not meet the specifications within this document.

##### 1.1 REFERENCES

{NOTE:  users of this specification should modify this section to suit specific project details.}

- ASTM D1622 Apparent Density of Rigid Cellular Plastics

- ASTM C165 Measuring Compressive Properties of Thermal Insulations

- ASTM  C203 Breaking Load & Flexural Properties of Block-Type Thermal Insulation

- ASTM C303 Dimensions & Density of Preformed Block & Board-Type Thermal Insulation

- ASTM C518 Steady-State Thermal Transmission Properties by Means of the Heat Flow Meter Apparatus

- ASTM D1621 Compressive Properties of Rigid Cellular Properties

- ASTM D1761 Mechanical Fasteners in Wood

- ASTM D1929 Determining Ignition Temperatures of Plastics

- ASTM D2126 Response of Rigid Cellular Plastics to Thermal & Humid Aging

- ASTM D2842 Water Absorption of Rigid Cellular Plastics

- ASTM D2843 Density of Smoke from the Burning or Decomposition of Plastics

- ASTM D2863 Limiting Oxygen Index

- ASTM D635 Rate of Burning &/or Extent & Time of Burning of Plastics in a Horizontal Position

- ASTM D638 Tensile Properties of Plastics

- ASTM D732 Shear Strength of Plastics by Punch Tool

- ASTM E119 Fire Tests of Building Construction & Materials

- ASTM E96 Water Vapor Transmission of Materials

- CCMC Masterformat 03131

- UBC 26-3 Room Fire Test Standard for Interior of Foam Plastic Systems

- ASTM E84 Surface Burning Characteristics of Building Materials

- ACI 318 (or CAN 3A23.1) Building Code Requirements for Structural Concrete with Commentary.

- ACI 347R Guide to Formwork for Concrete

- ACI 301 Structural Concrete for Buildings

- ASTM E2634 Standard Specification for Flat Wall Insulating Concrete Form (ICF) Systems

- QAI Evaluation to IBC and IRC 2012

- Greenguard Indoor Air Quality Certificate of Compliance certificate no. 38-00

- City of Los Angeles Research Report No. 25518

- Wisconsin Building Products Evaluation Report No. 200721-I

- Florida Product Approval No. FL14109

- Miami-Dade County NOA No.09-0714.03

- City of New York MEA 273-04-M

- QAI Fire Resistance Ratings, per ASTM E119

##### 1.2 DEFINITIONS

- Wall Alignment System - bracing that acts as an alignment/scaffold system designed for use with XP-1.

- Installing Contractor – A contractor contracted to install XP-1, and who has training and experience in the installation of one-sided ICF form systems.

- Technical Advisor – An individual who has the training and experience to assist in the installation of one-sided ICF form systems.  The role of the Technical Advisor shall be as technical support to the Installing Contractor.  The Technical Advisor may be a representative of the distribution firm or LOGIX ICF.

- EPS - Acronym for “Expanded Polystyrene”, the foam component of the XP-1.

- Plywood forms – The temporary wood wall form component of the XP-1.

- Polypropylene webs – The tie component of the XP-1.

- ICF - Acronym for “Insulated Concrete Form”.

- One-sided ICF – Where the forming systems consists of ICF on one side of the wall, while the other side of the wall consists of temporary wall forms to allow for exposed concrete.

- Service Penetrations – services such as electrical wiring, pipes, ventilation systems, etc.that are installed in or through the LOGIX ICF walls.

  - SYSTEM DESCRIPTION

- XP-1 system shall consist of flame-resistant EPS boards, and removable plywood wall forms, that are separated by polypropylene webs.  The EPS boards shall be manufactured using {BASF Neopor bead resins} {BASF bead resins}.

- XP-1 system shall be used as a one-sided ICF form, or in combination with solid form units (LOGIX PRO) or knock-down forms (LOGIX KD) or a combination of both LOGIX PRO and KD forms, referred to as LOGIX Hybrid Forms.

- The EPS shall be minimum 2.75 inch (70 mm) thick, which gives a total EPS foam board thickness of 5.50 inches (140 mm).  EPS panel inserts of varying thickness shall be used within the XP-1 cavity to allow for higher insulation values.

- The webs shall separate the EPS and the plywood forms, to form common concrete thicknesses of 4 inch to 14.75 inch.  Wider thickness shall be created using Logix Tie Xtenders.

- The volume of webs within the concrete wall component shall be no more than 0.25%.

- The webs shall be spaced minimum every 8 inch (203 mm) on centre horizontally and 16 inch (406 mm) on centre vertically, and contain a 1.25 inch (32 mm) wide furring strip that extends the height of each XP-1 EPS panel.  The furring strips shall facilitate fasteners for attachment of both exterior and interior finishes.

- A furring strip shall be located in the corners of forms.  The furring strip shall consist of both a vertical and horizontal component.  The vertical component shall extend nearly the full height of the form, extend a minimum of 2.5 inches (64 mm) from both sides of the corner, and a minimum of 0.2 inches (5 mm) thick.  The horizontal component shall be minimum 2 inches (51mm) in height, extend a minimum of 6 inches (152 mm) from both sides of the corner, and a minimum of 0.2 inches (5 mm) thick.

- The webs facilitate rebar placement in accordance with ACI 318.

1.3.1 Design/Performance Requirements

{NOTE:  users of this specification should modify this section to suit specific project details.}

{NOTE:  Additional design/performance information, as required, can be obtained by contacting LOGIX at info@logixicf.com}

- {Minimum thermal resistance of XP-1 Platinum EPS form panels shall be R4.71}

- {Minimum thermal resistance of XP-1 PRO EPS form panels shall be R4.13}

- Fasteners to be used for attachment of exterior cladding to ICF shall demonstrate, by either testing or engineering principles, resistance to design wind loads.

- Compliance to ASTM E2634, “Standard Specification for Flat Wall Insulating Concrete Forms.”

1.4 SUBMITTALS

- Relevant data for submission before, during and after construction include the following:

- Laboratory tests or data that validate product compliance with performance criteria specified, including standards and evaluations listed in Section 1.1, References;

- Relevant code compliance certificates including standards or evaluations listed in Section 1.1, References

- Manufacturer’s Product/Design or Installation Manual

- Product drawings showing dimensions, wall section course heights, layout, form types and details.

1.4.1 Quality Assurance

{NOTE:  This section may be modified to suit specific project details.}

- The Installing Contractor shall comply with all requirements, but not limited to, as outlined in this section.

1.4.1.1 Qualifications

- Installing Contractor shall be ICF trained and experienced.

- Installers of XP-1 shall provide proof of training documentation to contractor.

- A XP-1 Technical Representative shall be available to supervise construction on a regular basis.

1.4.1.2 Regulatory Requirements

- Installing Contractor including trades working under the Installing Contractor shall comply with local building code and regulatory requirements.

- Installation of XP-1 shall comply with ACI 347.

1.4.1.3 Field Samples

- Installing Contractor shall provide field samples, if required.  The samples will be physical examples illustrating finishes, coatings, or finish such as concrete, brick or stone.

1.4.1.4 Mock-Ups

- If required by owner, full-size assemblies of a wall assembly shall be constructed for review of construction, coordination of the work specified, testing, operation and training of the trades.  The mock-up can form part of the finished work if approved by the owner.

1.4.1.5 Pre-installation Meetings

- The Installing Contractor shall meet with the Contractor and relevant trades, as required, to coordinate the delivery, storage and handling of XP-1 including XP-1 components.

1.5 DELIVERY, STORAGE & HANDLING

1.5.1 Packing, Shipping, Handling & Unloading

- XP-1 shall be delivered on-site in original factory packaging.  All delivered XP-1 products shall show traceability by bearing on the identification label the location of manufacturing plant, product description, batch/lot number and date produced.

- Care shall be exercised in handling and unloading XP-1 onto the construction site to minimize damage to the EPS panels and/or webs.  XP-1 shall remain in original factory packaging until ready for installation.

- Storage location shall be in an area that will minimize damage or soiling to XP-1 products.  Protection shall be provided in cases where stored products of XP-1 could be exposed, for more than 2 weeks, to UV or freezing rain or snow conditions.

1.6 PROJECT CONDITIONS

{NOTE:  If appropriate, include additional relevant specific site conditions}

See above section.

1.7 SEQUENCING

{NOTE: This section is optional.  State in this section, if appropriate, requirements for coordinating work that requires unusual scheduling with work in another section.  The particular schedule of events should be specified here.}

1.8 WARRANTY

{NOTE: Contact manufacturer for details of warranty and describe in this section.}

1.8.1 Special Warranty

{NOTE: Include statements specific to this section which supplement or extend the warranty.}

| PART 2 PRODUCTS 2.0 MANUFACTURERS Insulating concrete forming products and accessories shall be manufactured by LOGIX. 2.1 MATERIALS Insulating concrete forms shall be made with {BASF Neopor EPS for XP-1 Platinum }{BASF EPS for XP-1}. Web ties and furring tabs shall be made with polypropylene plastic meeting the requirements in Section 1.3, 1.4 and Part 2. |  |
| --- | --- |

2.3 CONCRETE & REINFORCING STEEL

- Concrete slump shall be 5 to 7 inches (127 to 178 mm).  Slump may differ depending on design revisions to suit application.

- Reinforcing steel shall be as specified under Section 03 20 00, and as required by the design engineer.

- Structural design of reinforced concrete shall comply with ACI 318 & 301 as applicable.

2.4 WALL ALIGNMENT AND SCAFFOLDING SYSTEM

- The Wall Alignment and Scaffolding System shall be used as a wall bracing system, and consist of an adjustable mechanism to ensure, and maintain, plumbness of the wall during construction.  Installation of XP-1 shall comply with ACI 347R.

- Assembly of the wall alignment and scaffolding system shall comply with local building and regulatory codes.

- The wall alignment and scaffolding system shall be assembled to handle all design construction loads, and must be approved by a design engineer.

- The wall alignment and scaffolding system shall demonstrate resistance to the following design load conditions:

- Design wind load of 90 mph unoccupied, and 35 mph occupied, in accordance with ASCE 7-98 “Minimum Design Loads for Buildings and Other Structures”, and the “Tilt-up Concrete Association’s Guideline for Temporary Wind Bracing of Tilt-up Concrete Panels During Construction.”

- Light-duty loading of 25 psf, as specified by OSHA.

- Horizontal loading of 200 lb applied at the top rail to simulate a worker leaning against the guardrail.

2.5 WATERPROOFING

- Waterproofing shall be installed as specified under Division 07 00 00.

- Where called for on drawings, waterproofing against the EPS shall be an EPS compatible waterproofing system approved by the owner’s Engineer or Architect.

2.6 PARGING

- Where parging (stucco type) is required, supply & installation of parging shall be as specified under Section 09 24 00, Portland Cement Plaster.

- Alternate EIFS coatings shall be supplied and installed under Section 07 24 00, EIFS Systems.

2.7 STRUCTURAL METAL PANELS

- For the use of Structural Metal Panels over the EPS side of XP-1 panels, ICF Dead and Construction load anchor points shall be defined, if required by the Structural Metal Panel manufacturers.

- The location of the ICF Connectors/Dead and Construction load anchors shall be coordinated by the Architect/General Contractor with the ICF Manufacturer, and the Metal Panel Manufacturer.

- Panel subframing shall be fastened to the concrete.

## 3 EXECUTION

3.0 EXAMINATION

- Special attention shall be paid to assessing all areas of work to determine, as much as possible, the scope of work involved.

3.1 SITE VERIFICATION OF CONDITIONS

- The Installing Contractor shall verify the following site conditions prior to installation of XP-1:

- Site access and egress;

- Site conditions are as set out in Section 1.6 Project Conditions;

- Footings installed under Section 03 30 00 are within +/- ¼ inch (6 mm) of level and that steps in footings are 16 inches (406 mm) in height;

- Reinforcing steel dowels are in place at specified centers along footing lengths.

3.2 PREPARATION

- The Installing Contractor shall ensure top of footings are clear of debris prior to installing XP-1.  All debris must be removed from the interior of the forms prior to installation.

3.3 INSTALLATION

- Installation of XP-1 shall be in conformance to the Installation Manual or as per the Technical Advisor’s recommendations.  Alternate installation methods shall be approved by the owners’ engineer.

- The Installing Contractor shall ensure the proper installation methods for the following work are employed on site.  The installation method shall comply with the manufacturer’s installation instructions, unless alternate methods are approved by the owner’s engineer.

- Installation of First Course

- Installation of Reinforcement

- Setting Successive Courses

- Installation of plywood wall forms

- Forming Door & Window Openings

- XP-1 Alignment & Scaffolding System Installation

- Inspection and alignment of forms Prior to Concrete Placement

- Concrete Placement

- XP-1 Alignment & Scaffolding System Removal

  - SERVICE PENETRATIONS

- Service penetrations shall be installed where indicated on approved

- Service penetrations shall be installed by the appropriate trade.

- Where service penetrations run through the XP-1 wall, sleeves shall be provided to create a void where the service is to be located.  Sleeves shall be placed prior to concrete placement.

  - CONCRETE PLACEMENT

- Concrete placement shall not exceed a pour rate of 4 ft/hr.

- Maximum pour height shall not exceed 14 ft.  In addition, XP-1 shall demonstrate resistance to the lateral concrete pressure exerted from placing concrete in a 14 ft tall wall, per ACI 347, “Guide to Formwork for Concrete.”

3.6 FIELD QUALITY CONTROL

- The Installing Contractor shall inspect the erected formwork prior to placing concrete.  The formwork shall be inspected to verify, but not limited to, the following:

- Conformance to design drawings;

- Plumbness of wall;

- Rebar placement;

- Stability of wall alignment system (wall bracing system) and any additional anchoring system required to keep the walls aligned position and rigidity.

3.7 CLEANUP

- Installing Contractor shall ensure his/her work site is kept clean always.  All material shall be properly disposed, and all remaining debris shall be removed from the work site following the complete installation of XP-1.

3.8 PROTECTION

- Prior to concrete placement, interlocking knobs along the top of the EPS panels shall be protected with tape or other means to ensure no concrete debris sets on and between the interlocking knobs.

- Protection of installed EPS panels shall be provided if the forms are expected to be exposed to UV rays for longer than 180days (i.e. delay in final wall finish application).

- See Section 1.5.1 for additional protection requirements.

END OF SECTION